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	PRODUCT SPECIFICATION
	ARTICLE

OS5345-3B  S3  BLACK

	
Article                       OS5345-3B  S3  
Weight                      1,120 Kg SIZE 42
  Color                        BLACK
	
Description of the article: safety shoe, ankle model, full grain  leather, lining CAMBRELLA, double density outsole in Pu, steel toe cap toecap and steel  midsole. 
	SECURITY CATEGORY
S3SRC

	TECHNICAL DETAILS
	IMAGE 

	Type of PPE 
	Safety shoe for professional use in compliance with low EN ISO 20345:2011
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	Main features
	Black anklemodel of safety shoe in printed leather, 
Double layer sole in soft latex, antistatic, anti bacterial with SANITIZED treatment, lined in breathable and high scratch resistant fabric.
Mesh Cambrella lining, good breathable.
grey  stitching.
Black-grey laces  
Steel  toecap, resistant up to 200 J.
Steel   midsole,.
Test results: resistance improved more than 20% to nail's Perforation (diameter 4,5mm) comparable to a strength of 1360 N instead of 1100 N requested by EN 12568. 
Double density outsole, antistatic, anti spilt, resistant to oil spilt and, injected on the upper.
- First injection in PU of grey color. Shock absorber main features.             
-  Land outsole very resistant in PU..             
	

	Security category 
	S3
	

	Law
	CE UNI EN ISO20345:2011 – SAFETY SHOES 
	

	Main features 
	UNI EN ISO 20345:2011 – Safety shoe with toe capacity resistance  up to 200 J 
ENV 13287:2000 – Anti slip resistance
Directive 1907/2006/CE –  Determination of dangerous substances for leather and fabric elements. 
Directive  1907/2006/CE  – Determination of the level of nickel for the metal parts in contact with the foot. 
	

	
	This safety shoe S3SRC is in compliance with the law  EN 20345:2011  

	

	Manufactured by
	CALZATURIFICIO 5BI-ITALY
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